## Slide 1: Toyo Ink America’s PSA’s for Low VOC Automotive Applications - 2021
Excellent adhesion to automotive FOAMS
Great heat resistance and shear
Meet low VOC automotive specs (Toluene free PSA)
PSA |  | BPS 5375TX | BPS 6080TX | BPS 6574TX | BPS 6391TX
Concept |  | STD | Toluene free | High solid Toluene free | High solid Toluene free
Solid content |  | 45% | 45% | 57% | 70%
Viscosity (mPa･s) |  | 8,000 | 8,500 | 7,000 | 7,000
Type |  | 2 parts | 2 parts | 2 parts | 2 parts
24hr Peel at 23℃50%RH (lb/inch) | to SS | 5.4 | 5.5 | 5.8 | 5.5
 | to PE | 2.3 | 2.4 | 2.4 | 2.2
Shear 1kg-80℃-70,000sec |  | Pass | Pass | Pass | Pass
FOAM sheet 2” Mandrel test | 23℃ (73F) | No flagging | No flagging | No flagging | No flagging
 | 69℃ (156F) | No flagging | No flagging | Limited flagging | Limited flagging
Base material ： PET50μm Coating weight ： 50 g/m2
PSA |  | BPS 6574TX | BTX-275 |  | BPS 6080TX | BTX-136
Concept |  | High solid Toluene free | Improved of BPS6574TX Better VOC |  | Toluene free | Improved of BPS6080TX Best VOC
Solid content |  | 57% | 57% |  | 45% | 54%
Viscosity (mPa･s) |  | 7,000 | 5,000 |  | 8,500 | 8,000
Type |  | 2 parts | 2 parts |  | 2 parts | 2 parts
24hr Peel at 23℃50%RH (lb/inch) | to SS | 5.8 | 5.8 |  | 5.5 | 5.7
 | to PE | 2.4 | 2.2 |  | 2.4 | 2.2
Shear 1kg-80℃-70,000sec |  | Pass | Pass |  | Pass | Pass
Ball tack (J. Dow Method) | (#) | 5 | 6 |  | 7 | 6
Excellent adhesion to automotive FOAMS
Reduced Low volatiles & Odor factor substances
Excellent performance in Fogging test
Application